客 户                            日期   2021-12-30

#### CUSTOMER   湖南栋阳精密科技              DATE

#### 认 可 书 # SPECIFICATION FOR APPROVAL

`

| 客户品名 CUSTOMER P/N | ## PC44 ED27-30 |
| --- | --- |
| 康明品名 P/N | PC44 ED27-30 |
| 认可书编号 SPEC.NO. |  |

客户认可APPROVED BY： (为保证订单顺利,请在1个月内认可或回复) 如有客户品码(料号),请填写在下 客户品码(料号):

| 批准 APPROVED BY | 审核 CHECKED BY | 拟制 PREPARED BY |
| --- | --- | --- |
| 严晓明 |  | 张霞萍 |

#### 认 可 书 # SPECIFICATION FOR APPROVAL

| 客户 CUSTOMER: |  |  | P/N | ### ED27-30 |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | SPEC./N |  |  |
| Ⅰ.更改记录 REVISION RECORD: |  |  |  |  |  |
|  | 版本号 REV NO | 更改内容及原因 CONTENTS AND REASONS | 日期 DATE OF APPROVAL |  | 担当 DRAWN |

| 1. 尺寸DIMENSIONS(mm) 尺寸 DIMENSIONS(mm). A; 27.3±0.4. B; 6.5±0.2. C1; 30.15±0.5. C2; 25.1±0.4. D1; 22.7±0.5. D2; 19.45±0.5. E; 7.15±0.2. F; 3.8±0.2. 底; 2.5±0.2. 磁芯参数 CORE PARAMETERS. 有效磁路长度Effective Length Le; 39.3 (mm). 有效截面积Effective Cross Area Ae; 151.03 (mm2). 有效体积Effective Volume Ve; 5935.51(mm3). 重量Approx. Weight (g); (g/set). |
| --- |
| Item: | P/N: | SPEC./N |
| FERRITE CORE | ED27-30 |  |

2. 电气特性 ELECTRICAL CHARACTERISTICS

| 项目 ITEMS | 规格 SPEC | 测试条件 TESTING METHOD | 测试仪器 TESTING INSTRUMENT |
| --- | --- | --- | --- |
| 电感 INDUCTANCE | AL:3500±25%nH/N2 | 1kHz,0.3V,23±3℃ | HP4284 OR YD2810 |
| 功率损耗 POWER LOSS | PL:≤500mW/cm3 | 100kHz,200mT,100±3℃ | SY8232 OR CH258 |
| Q值 Q VALUE |  |  | HP4284 OR YD2810 |
| 直流叠加LDC DC SUPERPOSITION LDC |  |  |  |
| 阻抗Z IMPEDANCE Z |  |  |  |

3.材质特性MATERIAL CHARACTERISTICS

材料 MATERIAL：

| 特性 CHARACTERISTICS |  |  | 单位UNIT |  | 特性质VALUE |
| --- | --- | --- | --- | --- | --- |
| 初始磁导率 INITIAL PERMEABILITY μi |  |  | ＿ |  | 2300±25% |
| 饱和磁通密度SATURATION MAGNETIC FLUX DENSITY (H=1194A/m) Bs |  | 25℃ | mT |  | 510 |
|  |  | 100℃ |  |  | 390 |
| 剩余磁通密度 REMANENT FLUX DENSITY Br |  | 25℃ | mT |  | 100 |
| 矫顽力 COERCIVE FORCE Hc |  | 25℃ | A/m |  | 14 |
| 比损耗因子 RELATIVE LOSS FACTOR Tanδ/ui |  |  | ＿ |  |  |
| 初始磁导率比温度系数 RELATIVETEMP.FACTOR αuir |  |  | ＿ |  |  |
| 居里温度 CURIE TEMP. Tc |  |  | ℃ |  | 220 |
| 电阻率 ELECTRICAL RESISTIVITY ρ |  |  | Ω/m |  | 6.5 |
| 密度 DENSITY d |  |  | kg/m3 |  | 4.8 |
| Item: | P/N: |  |  | SPEC./N |  |
| FERRITE CORE | ED27-30 |  |  |  |  |

4.允许最大缺陷（外观）Maximum chip off:

- 磁芯配合面上裂缝深度不超过0.3mm，长度不超过延长线长度的1/4,磁芯非配合面上裂缝深度不超过0.5mm，长度不超过延长线长度的1/3

The depth of crack in the ground surface should be no more than 0.3mm, length is no more than 1/4 length of lengthen line. In the non-ground surface, the depth should be no more than 0.5mm length is no more than 1/3 length of lengthen line.

- 对于磁芯的外观检验方面，执行如下标准规格：

|  |  | 接合面 | 其他表面 |
| --- | --- | --- | --- |
| 破损 | 1处破损的面积 | ≤0.7mm2 | ≤1.0mm2 |
|  | 2处以上破损面积的合计 | ≤2.0mm2 | ≤5.0mm2 |
|  | 破损深度 | ≤0.7mm | ≤1.0mm |
| 其他 | 实际使用中无有害毛刺，裂纹，气孔等 |  |  |

5.检验方法（Inspection Method）:

按GB/T2828.1-2003，一次正常抽样，检查水平Ⅱ，ＡＱＬ符合下列标准。

According to GB/T2828.1-2003.one time normal random sampling,Inspect level Ⅱ,AQL.should be as follows;

|  | 合格质量水平AQL | 检查项目Inspect Item |
| --- | --- | --- |
| A | 0.65 | 电磁特性Electromagnetic Property |
| B | 1.0 | 外形尺寸Outside Size |
| C | 1.5 | 外观质量Outside Quality |

6.包装Packing:

内包装采用泡塑盒，外包装采用纸箱，每箱产品外面都贴上产品合格证（包括品名、数量、批号、检验员）。

Foamed plastic box is used to inside packing,paper box is used to outside packing,Qualify Certification is attached on every  box,including Item (Product name or type),Quantity,Lot No.and Tester.

| Item: | P/N: | SPEC./N |
| --- | --- | --- |
| FERRITE CORE | ED27-30 |  |