客	户	日	期

CUSTOMER	通用		DATE	2021.2.4

书

APPROVAL

SPECIFICATIONFOR

可

认

`

| 客 户 品 名 C U S T O M E R P / N | PC95 - PQ18.2 |
| --- | --- |
| 宇 通 品 名 P / N | PC95 - PQ18.2 |
| 认 可 书 编 号S P E C . N O . | YT C R 2 0 2 1020401 |

客 户 认 可 A P P R O V E D	B Y ：

( 为 保 证 订 单 顺 利 , 请 在 1 个 月 内 认 可 或 回 复 )

如 有 客 户 品 码 ( 料 号 ) , 请 填 写 在 下客 户 品 码 ( 料 号 ) :

海 宁 市 康 明 电 子 有 限 公 司

| 批准APPROVED BY | 审核CHECKED BY | 拟制PREPARED BY |
| --- | --- | --- |

SPECIFICATIONFORAPPROVAL

书

可

认

客户 CUSTOMER: 	通用

P/N SPEC./N0

PC95-PQ18.2

Ⅰ.更改记录 REVISION RECORD:

版本号REV NO

更改内容及原因CONTENTS AND REASONS

日期

DATE OF APPROVAL

担当DRAWN

| 1. 尺寸DIMENSIONS(mm) 尺寸 DIMENSIONS(mm). A; 18.2±0.3. B; 5.75±0.25. C; 12.7±0.2. D; 7.9±0.15. E; 14.7±0.3. F; 3.6±0.25. B-F; 2.15±0.2. 磁芯参数 CORE PARAMETERS. 有效磁路长度Effective Length Le; 27.9mm. 有效截面积Effective Cross Area Ae; 51.1mm ². 有效体积Effective Volume Ve; 1427.6mm ³. 毛坯重量Approx. Weight (g); 9g. 气隙值GAP(mm); 0mm. |
| --- |
| Item: | P/N: | SPEC./N |
| FERRITE CORE | PC95-PQ18.2 |  |

2. 电气特性 ELECTRICAL CHARACTERISTICS

| 项目 ITEMS | 规格 SPEC | 测试条件 TESTING METHOD | 测试仪器 TESTING INSTRUMENT |
| --- | --- | --- | --- |
| 电感 INDUCTANCE | AL=3000nH/N2±25％ | 1kHz, 0.3 V,23±3℃ 10Ts | HP4284 OR YD2810 |
| 功率损耗 POWER LOSS | ①PL:≤580mW/cm3 ②PL≤580mW/cm3 | 100kHz,200mT,10Ts ①.25±3℃②.100±3℃ | SY8232 OR GHY-5 |
| Q值 Q VALUE |  |  |  |
| 直流叠加LDC DC SUPERPOSITION LDC |  |  |  |
| 阻抗Z IMPEDANCE Z |  |  |  |

3.材质特性MATERIAL CHARACTERISTICS

材料 MATERIAL：PC95

| 特性 CHARACTERISTICS |  |  | 单位UNIT |  | 特性质VALUE |
| --- | --- | --- | --- | --- | --- |
| 初始磁导率 INITIAL PERMEABILITY μi |  |  | ＿ |  | 3200±25% |
| 饱和磁通密度SATURATION MAGNETIC FLUX DENSITY (H=1194A/m) Bs |  | 25℃ | mT |  | 510 |
|  |  | 100℃ |  |  | 390 |
| 剩余磁通密度 REMANENT FLUX DENSITY Br |  | 25℃ | mT |  | 85 |
| 矫顽力 COERCIVE FORCE Hc |  | 25℃ | A/m |  | 8 |
| 比损耗因子 RELATIVE LOSS FACTOR Tanδ/ui |  |  | ＿ |  |  |
| 初始磁导率比温度系数 RELATIVETEMP.FACTOR αuir |  |  | ＿ |  |  |
| 居里温度 CURIE TEMP. Tc |  |  | ℃ |  | 215 |
| 电阻率 ELECTRICAL RESISTIVITY ρ |  |  | Ω/m |  | 6.5 |
| 密度 DENSITY d |  |  | kg/m3 |  |  |
| Item: | P/N: |  |  | SPEC./N |  |
| FERRITE CORE | PC95-PQ18.2 |  |  |  |  |

PC95曲线图

- Pcv-Bm                                          μi-T

B-H                                           Pcv-T

| Item: | P/N: | SPEC./N |
| --- | --- | --- |
| FERRITE CORE | PC95-PQ18.2 |  |

5.允许最大缺陷（外观）Maximum chip off:

- 磁芯配合面上裂缝深度不超过0.3mm，长度不超过延长线长度的1/4,磁芯非配合面上裂缝深度不超过0.5mm，长度不超过延长线长度的1/3

The depth of crack in the ground surface should be no more than 0.3mm, length is no more than 1/4 length of lengthen line. In the non-ground surface, the depth should be no more than 0.5mm length is no more than 1/3 length of lengthen line.

- 对于磁芯的外观检验方面，执行如下标准规格：

|  |  | 接合面 | 其他表面 |
| --- | --- | --- | --- |
| 破损 | 1处破损的面积 | ≤0.7mm2 | ≤1.0mm2 |
|  | 2处以上破损面积的合计 | ≤2.0mm2 | ≤5.0mm2 |
|  | 破损深度 | ≤0.7mm | ≤1.0mm |
| 其他 | 实际使用中无有害毛刺，裂纹，气孔等 |  |  |

5.检验方法（Inspection Method）:

按GB/T2828.1-2003，一次正常抽样，检查水平Ⅱ，ＡＱＬ符合下列标准。

According to GB/T2828.1-2003.one time normal random sampling,Inspect level Ⅱ,AQL.should be as follows;

|  | 合格质量水平AQL | 检查项目Inspect Item |
| --- | --- | --- |
| A | 0.25 | 电磁特性Electromagnetic Property |
| B | 0.65 | 外形尺寸Outside Size |
| C | 1.0 | 外观质量Outside Quality |

8.包装Packing:

内包装采用泡塑盒，外包装采用纸箱，每箱产品外面都贴上产品合格证（包括品名、数量、批号、检验员）。

Foamed plastic box is used to inside packing,paper box is used to outside packing,Qualify Certification is attached on every  box,including Item (Product name or type),Quantity,Lot No.and Tester.

| Item: | P/N: | SPEC./N |
| --- | --- | --- |
| FERRITE CORE | PC95-PQ18.2 |  |